# THE EVOLUTION OF SUBSTRUCTURE IN 50%Ni+50%Nb POWDER MIXTURE DURING BALL MILLING.

## A.N.Ivanov, T.A.Sviridova, E.V.Shelekhov.

## Moscow Steel and Alloys Institute

### Introduction.

Nanocrystalline (nc) materials have attracted interest recently as they contain a large volume fraction of grain boundaries, which lead to novel properties. Characterization of nc materials substructure, such as grain size and root mean square strains, is important for both fundamental and practical purposes. Sample preparation for X-ray diffraction (XRD) studies is simple, and averaging over many grains is produced automatically. Therefore XRD has been preffered over TEM in the nc materials substructure analysis.

The Warren-Averbach method [1] has been employed to study substucture evolution in Ni and Nb in the course of ball milling of both the annealed elemental powders and their equiatomic mixture.

### Experimental procedures.

Ball milling (planetary mill of AGO-2U type was used) at energy intensity ~5 Wt/g has been performed for 10160 min. Milling vials were filled and sealed in Ar atmosphere. XRD patterns have been taken with CoK- and CuK-radiation using monochromated diffraction beam and step scanning DRON-4 diffractometer. We recorded 111-222 (Ni) and 110-220 (Nb) line profiles in order to find the area-averaged grain size D (column length), the grain size distribution function p(L) and the rms (L)=(<2(L)>)½. The "hook effect correction" procedure described in [2] has been applied to calculate D and p(L).

### Experimental results.

1. Average grain size.The area-averaged nc grain size D after different milling time are presented in the table below.

D values (in nm) after ball milling at different time.

| Milling time, min | in Ni | in Nb |
| --- | --- | --- |
| 10 | 33.9 ± 1.5 | 20.1 ± 1.2 |
| 15* | 16.0 ± 1.5 | 9.0 ± 1.0 |
| 20 | 21.3 ± 1.2 | 16.6 ± 1.0 |
| 30* | 12.0 ± 1.5 | 8.5 ± 1.0 |
| 40 | 14.7 ± 0.8 | 14.7 ± 0.8 |
| 80 | 11.6 ± 0.6 | 8.8 ± 0.6 |
| 160 | 16.4 ± 1.0 | 9.8 ± 0.6 |

*)milling of 50%Ni+50%Nb mixture

The nc grain size in Ni and Nb gradually decreases with milling duration of elemental powders. In Nb grain refining proceeds slower than in Ni though the nc grains are finer. Average nc grain size grows a little in Ni when milling time raises from 80 to 160 min probably due to dynamical recovery process and cold welding of separate fine particles. The most pronounced is the fact of much faster nc grains refining in both Ni and Nb if the powder mixture has been milled instead of the elemental powders. Nevertheless, the minimum average grain size achieved is practically the same for the mixture and for the elemental powders.

2. Nc grain size distribution. Fig.1 shows the evolution of the distribution function p(L). In Ni as well as in Nb powders milled separately p(L) becomes narrower and shifts to smaller L-values as milling time increases. In Nb it goes gradually with time whereas in Ni after 160 min of milling the p(L) shifts to higher L and becomes broader comparing with 80 min milling. These effects coincide with the behaviour of D-values at the same milling time.

After 15 min of the powder mixture milling the distribution functions in both Ni and Nb resembles that of the elemental powders milled for 40 min. Mixture milling for 30 min produces similar both the grain size and the grain size distribution to 80 min milling of the appropriate elemental powder.

3. RMS evolution. After milling of the Nb elemental powder for 10-40 min the rms dependences on L are the same within the limit of errors. Then after 80-160 min of milling the rms-values become 1.5 times higher, Fig.2. In all cases of Fig.2 the data show good fitting by <2(L)>=A/L. The milling of the mixture exhibits nothing special for Nb: after 15 and 30 min the rms dependences on L pass between that of the elemental powders milled for 10-40 min and 80 min. These clearly indicate faster crystall defects formation in Nb on milling in the mixture as compared with the treatment of the elemental powder. In Ni the rms values grow with milling time up to 80 min (Fig.3) then they decrease after 160 min indicating probably the dynamical recovery process occured (compare with the change of D and p(L) at the same milling time).

However, the rms dependences on L in Ni milled in the mixture, unlike Nb, differ from that of the milled elemental Ni powder, Fig.3b. After 15 min of milling the rms values are lower them the values for 10 min milled elemental powder. After 30 min of milling the rms dependence is similar to that after 15 min but the values are 1.5 times higher and it coincides with the one observed for 20 min milled elemental powder.

### Conclusions

In the course of elemental powders ball milling nc substructure is formed in Ni and Nb with the average grain size after 80 min of treatment equal to 12 and 9 nm respectively. It is coupled with the narrowing and shift to smaller L values the grain size distribution function and with the increase of the rms.

The milling of 50%Ni+50%Nb mixture exhibits, in general, the same features of substructure evolution in Ni and Nb though it proceeds remarkably faster due to the solid state reaction (amorphization) which is practically completed after 60 min of milling because of the high chemical affinity of these elements.

### Literature

[1]. B.E. Warren. X-ray Diffraction. Massachusetts: Adison-Wesley, 1964, chapter 13.

[2]. H.H. Tian, M.Atzmon. Comparison of x-ray analysis methods used to determine grain size in nanocrystalline materials. Phil.Mag.(A) to be published in 1999.

a

b

Fig.1. The nc grain size distribution functions p(L) after different milling time for Ni milled elemental powder (a); Nb milled elemental powder (b)

c

d

Fig.1. The nc grain size distribution functions p(L) after different milling time for Ni milled in mixture (c); Nb milled in mixture (d)

Fig.2. The rms, (L), dependence on L for Nb milled as elemental powder (a); milled in mixture (b).

a

b

a

b

Fig.3. The rms, (L), dependence on L for Ni milled as elemental powder (a); milled in mixture (b).

b

a

Fig.2. The rms, (L), dependence on L for Nb milled as elemental powder (a); milled in mixture (b).

Fig.3. The rms, (L), dependence on L for Ni milled as elemental powder (a); milled in mixture (b).

a

b